WEST SYSTEM V-FLOOR LEVELLING TECHNIQUE

This technique for pouring a level mounting block on a V-floor appeared in “DIY Boat Owners Magazine” #4, 2006: www.diy-boat.com. It was reprinted by West Systems Inc: ”Casting a level Deck Fitting Base”, in “EPOXYWORKS #25, Summer 2007. It is a simple, straight forward method for creating a flat mounting platform on a V-floor.

Use a large milk carton, plastic bowl or other appropriate flat-bottomed container for casting the blocks. Spray the inside with non-stick cooking spray or apply paste wax to prevent the epoxy from bonding to the container.

MIX WEST SYSTEM EPOXY with 404 filler - to a stiff ketchup consistency and add SLOW HARDENER, as directed on the product sheets. The 404 filler dissipates the heat of cure. It is best to complete the shelf with several small pours, rather than a single large pour. Be sure that the last pour comes well below the container top, to avoid spilling over. MEASURE & MARK the fill line on each container, to be sure that the height of both blocks will be the same.

Place the containers at the exact spot that each mount is to be fixed prior to the first pour. When completed and cured, remove the block.

Turn the block over, remove the casting from the container and sand the tilted surfaces, MASK & then sand the floor in the masked off area.

Epoxy the blocks to the floor inside the prepped areas. The tops will be level.